## Slide 1: Measuring Dry Film Thickness (DFT) on Concrete Substrates
Craig Woolhouse
Elcometer UK

## Slide 2: DFT on Concrete Substrates
Traditional measurement techniques
Advances in NDT measurement technology
Use of the Elcometer 500 Coatings on Concrete Gauge
Things to look out for when measuring the coating thickness on concrete substrates
How to more effectively manage the results

## Slide 3: Traditional Measurement Techniques
Mechanical device – PIG Gauge
  Destructive
  Difficult to interpret results – scale range in the microscope

## Slide 4: Paint Inspection Gauge (P.I.G.)

## Slide 5: Current Measurement Techniques
Ultrasonic devices – Non Destructive

## Slide 6: Ultrasonic Measurement

## Slide 7: Ultrasonic Measurement
t is measured by the gauge
S is the calculated thickness
v (the velocity of the coating) is ‘inputted’ by the user
so if you set up the gauge with the wrong speed of sound, the thickness will be wrong

## Slide 8: Ultrasonic Measurement
t is measured by the gauge
S is the calculated thickness
v (the velocity of the coating) is ‘inputted’ by the user
Different coatings (Epoxy, Acrylic, PVC, rubber, etc) each have a different speed of sound, so for an accurate reading, you cannot simply have a single speed of sound for all coatings

## Slide 9: Ultrasonic Measurement
Metal Substrate DFT measurement isn’t daunting, so why should ultrasonic DFT be any different?
It doesn’t need to be. You shouldn’t have to set up gates or thresholds, or worry about what gain or what sort of A-Scan graph you have, the gauge should do this for you automatically
Calibrated correctly, the gauge should only give you the correct answer

## Slide 10: Ultrasonic Gauge Calibration
There are 4 options for calibrating an ultrasonic gauge
  Use a generic value for all coatings (not recommended)
  Select the appropriate coating from a pre-defined material selection (generic speed from pick list)
  Input the known speed of sound of the coating
  Measure a sample of known thickness

## Slide 11: Ultrasonic Gauge Calibration
There are 4 options for calibrating an ultrasonic gauge
  Use a generic value for all coatings (not recommended)
  Select the appropriate coating from a pre-defined material selection (generic speed from pick list)
  Input the known speed of sound of the coating
  Measure a sample of known thickness

## Slide 12: Ultrasonic Gauge Calibration
But how do you know what the speed of sound is for the coating?
Where do you get a sample of known thickness from?
A Coating Calibration Mould answers both of these questions. The CCM is a metal mould allowing for the creation of a known thickness of coating

## Slide 13: Ultrasonic Gauge Calibration
The CCM mould is filled with the coating under test
A scraper is used to level a predetermined wet film thickness of coating
Once fully cured a DFT gauge is used to accurately measure the coating thickness and …

## Slide 14: Ultrasonic Gauge Calibration
The ultrasonic gauge can now be calibrated accurately on a sample of known thickness
And used to determine the coating’s speed of sound, which can be stored in the gauge for later use, or used to calibrate other gauges

## Slide 15: Elcometer 500 Gauge Usage
Calibrate by setting the material speed of sound
Select the correct probe type (C1 or C2)
Take and store readings recognising that
  The gauge signal strength needs to be ‘in the green’
  If no reading occurs then carefully move the probe over the substrate until a reading is obtained
  Store the reading in the gauge memory
  Download the data to ElcoMaster

## Slide 16: Elcometer 500 Gauge Advantages
Fast
Rugged, Reliable and Ergonomic gauge design
Intelligent
  New probe tip is field replaceable
Ease of Use
  Simple Menu and On Screen Instructions
Powerful
  Connects to ElcoMaster reporting software

## Slide 17: Result Reporting
Ultrasonic measurement of coating thickness is covered by ASTM D6132-13 and SSPC-PA 9
These standards define the method, the procedure and the reporting requirements

## Slide 18: Result reporting to SSPC-PA 9
SSPC-PA 9 is a recommended procedure for measuring DFT using Ultrasonic Gauges
  a minimum of three (3) gage readings shall be made for each spot measurement of the coating.
  an area measurement is obtained by taking five (5) separate spot measurements each 10m2 up to 100m2
  For areas between 30 and 100m2 select 3 random 10m2 areas
  For areas greater than 100m2 measure as above for the first 100m2 and one 10m2 area per 100m2 thereafter

## Slide 19: Result reporting to ASTM D6132-13
ASTM requires the following to be reported
  Type of coating and substrate
  Instrument used
    manufacturer, model number, serial number and calibration date
  Type of coating thickness or reference standard
    Together with method of accuracy verification
  Mean and standard deviation of readings
  Operator I.D. and inspection date

## Slide 20: Result Reporting
Modern digital inspection gauges enable the operator to
  Save the readings in the gauge
  Transfer the readings from the gauge to the PC/Phone
  Analyse the data carrying out any calculations or statistical analysis required by the Standard
  Produce and email a report instantly

## Slide 21: Result Reporting
All the data required by the customer can be automatically transferred by the gauge to the software and directly onto your report… all at the click of a button

## Slide 22: Conclusion
You don’t need to panic at the mention of Ultrasonic DFT gauges as they don’t have to be complicated!
Measuring coatings on concrete has been made significantly easier, faster and more accurate with the introduction of new ultrasonic gauges and through the use of coating calibration moulds
Ultrasonic DFT results on concrete no longer need to be viewed with scepticism

## Slide 23
Now for a short demonstration…..