## Slide 1: Paperless Quality Assurance
Presenter:
Daniel Leonard
Customer Support Engineer
Elcometer Limited
© Elcometer Limited 2012
Notes: 1

## Slide 2: Paperless QA
Introductions

## Slide 3: Paperless QA
Objectives
  Measure surface profile using a digital surface profile gauge in accordance with ASTM D 4417 Method B (Elcometer 224)
  Measure for surface cleanliness using a salt contamination meter in accordance with SSPC Guide 15 ( Elcometer 130 )
  Measure ambient conditions in accordance with industry standards using a digital dew point meter (Elcometer 319)
  Measure dry film thickness using a type 2 gauge in accordance with SSPC-PA 2 and other major industry standards (Elcometer 456)
  Create a digital Coating Technical Report by importing your readings directly from each of the gauge types into Elcomaster 2.0

## Slide 4: Paperless QA
Course Outline
  Part 1: Measuring surface profile data using the Elcometer 224
  Part 2: Measuring surface salt contamination using the Elcometer 130
  Part 3: Measuring and recording climatic information using the Elcometer 319
  Part 4: Measuring dry film thickness using the Elcometer 456
  Part 5: Creating Paperless Quality Assurance reports with Elcomaster 2.0

## Slide 5: Paperless QA
Course Format
  Lecture
  Hands on practical sessions
    Elcometer 224
    Elcometer 130
    Elcometer 319
    Elcometer 456
    Downloading data from a gauge in Elcomaster 2.0
    Creating a simple report in Elcomaster 2.0
    Detailed report creation in Elcomaster 2.0
  Written test
    25 multiple choice questions
    Creation of a coating technical report

## Slide 6: Paperless QA
What is Paperless QA?

## Slide 7: Paperless QA
Paperless
QA
Quality Assurance: The maintenance of a desired level of quality in a service or product.
Quality is assessed and maintained through checks and inspections
Paper free. Carry out the procedure generating as few pieces of paper as possible.
Paper is easily lost and presents storage challenges

## Slide 8: Paperless QA
Elcomaster 2.0
Download data from complete
range of Elcometer gauges
Store and organise
gauge data along with other
photographs notes and reports in one
place
Create professional reports
using easy to design
templates
Create PDF report
files for easy printing
or emailing
Monitor gauges remotely
over bluetooth
Communicate your data
effectively to any level

## Slide 9: Paperless QA
Elcomaster 2.0 – Three key uses
A means of transferring data off the gauge, to store and to view
  Quick and easy record keeping

## Slide 10: Paperless QA
Elcomaster 2.0 – Three key uses
A means of transferring data off the gauge, to store and to view
  Quick and easy record keeping
Exporting the gauge data to excel
  Saves all batch readings and header data
  Keep records or do further spreadsheet analysis

## Slide 11: Paperless QA
Elcomaster 2.0 – Three key uses
A means of transferring data off the gauge, to store and to view
  Quick and easy record keeping
Exporting the gauge data to excel
  Saves all batch readings and header data
  Keep records or do further spreadsheet analysis
Creating professional, customised coating technical reports
  True paperless QA and record keeping
  No need for any other software

## Slide 12: Paperless QA
Coating technical report
The report contains all of the data collected during the coating application process
Gauge readings, specifications, inspection documents and photographs/diagrams may be included in the report
Data needs to be stored, organised and presented coherently

## Slide 13
Surface Preparation
Measuring blast profiles with the Elcometer 224

## Slide 14: Paperless QA
Module Objectives
  Define surface profile
  Define the surface profile coating requirements of related industry standards
  Measure surface profile using a digital surface profile gauge, in accordance with ASTM D 4417, Method B
  Download data from the Elcometer 224 gauge into Elcomaster

## Slide 15
  All materials have some kind of profile on the surface
  Large surface profiles are created during blasting
  The profiles created by grit, shot, garnet, copper slag will look and feel different even if the profile height is the same
Grit Shot
Paperless QA
Grit
Shot

## Slide 16: Paperless QA
  The roughened surface that results from abrasive blast or power-tool cleaning on bare metal
  For steel surfaces: A measurement of the peak-to-valley height of this roughness
  Often expressed as an average
  Typically ranges from 25 to 125 microns
  Profile depth can be varied in two ways
    Blast media
    Blast pressure
What is a blast profile?

## Slide 17
Promotes Adhesion
  Provides a “key” for the coating to cling to
  Too little profile – The coating will have poor adhesion and will fail prematurely
  Too much profile – More coating needed to fully cover the high peaks
  – Increased time to blast
  – Increased cost
  – Poor cure
  – Thinning of substrate
Removes some contamination
Paperless QA
Why create a blast profile?
Notes: 17
Surface preparation is the key to good anticorrosion coating performance. A paint will only stick to a surface if it is clean. One benefit of blast cleaning is that it leaves a profile which also enhances adhesion.
Elcometer is concerned with the assessment or measurement of profile and cleanliness and these are separate processes.

## Slide 18
Paperless QA
Increasing peak to valley profile
Notes: 18
Surface preparation is the key to good anticorrosion coating performance. A paint will only stick to a surface if it is clean. One benefit of blast cleaning is that it leaves a profile which also enhances adhesion.
Elcometer is concerned with the assessment or measurement of profile and cleanliness and these are separate processes.

## Slide 19: Paperless QA
How can it be measured?
  Comparators
    Quick way to characterise surface profile
    Potentially inaccurate, subjective
  Replica Tape
    Widely used established method
    Different grades required for different profiles
    Time consuming
  Surface profile gauges (Needle gauges)
    Fast, accurate method
    Generates paper, results normally recorded manually

## Slide 20: Paperless QA
  Digital surface profile gauge
  Available as standard and top models
  Standard and top models both come with statistics
  Top model stores data
  Compatible with Elcomaster 2.0
Elcometer 224
Notes: 20
This image shows the effect of the different cutter angles on the same thickness of coating.

## Slide 21: Paperless QA
Separate probes available with standard or armoured, reinforced heavy duty cables
Tungsten carbide user replaceable probe tips, suitable for up to 20,000 readings
Integral and separate gauges to measure surface profiles up to 500µm (20mils)
Fast reading rate of more than
60 readings per minute
Large easy to read
colour display
Scratch and solvent
resistant screen
Dust and water resistant
rugged design to IP64
USB and Bluetooth® data output to ElcoMaster™ 2.0 software
Large buttons with
positive feedback
Compatible with ElcoMaster™ for Android™
Auto rotating display with tap awake feature
Stores up to 150,000 readings in alpha numerical batches

## Slide 22
Advantages of Digital Profile Measurement
Accuracy
  Digital display
Speed
  Up to 60 readings per minute
  No calculation of averages necessary
Convenience
  Data can be stored in gauge and/or imported to Elcomaster 2.0 – Paperless QA
Paperless QA

## Slide 23: Counted Average Mode
The “Counted Average” feature on the new Elcometer 224 is a useful technique for assessing an area of profile.
To establish the average surface profile, between 5 and 10 readings should be taken within a 150 x 150mm (6 x 6”) area.
The average of these individual spot measurements provides the user with the peak-to-valley height over the measurement area.
The Counted Average records the average of the spot readings into the memory
Paperless QA

## Slide 24
Paperless QA
Demo: Opening a counted average batch

## Slide 25
Measurement Method
  Zero the instrument on toughened glass slide
  Open a new counted average batch in the 224
  Take an average of ‘x’ gauge readings as agreed or stated in the standard to produce a ‘measurement’.
  Readings or average of readings may be saved for download to Elcomaster 2.0
Paperless QA
Notes: 25

## Slide 26
Paperless QA
ASTM D4417 Method B
Provides a description of the techniques for measuring the profile of abrasive blast cleaned surfaces using a digital surface profile gauge. Suggests a mean value is taken as is average of 10 readings at each location. Then the mean for all surface locations is reported.
Surface profile test standards

## Slide 27
Paperless QA
ASTM D4417 Method B
Provides a description of the techniques for measuring the profile of abrasive blast cleaned surfaces using a digital surface profile gauge. Suggests one measurement is average of 10 readings
International Maritime Organization (IMO) Performance Standard for Protective Coatings (PSPC)
The measured profile should be between 30 and 75 microns
Surface profile test standards

## Slide 28
Paperless QA
ASTM D4417 Method B
Provides a description of the techniques for measuring the profile of abrasive blast cleaned surfaces using a digital surface profile gauge. Suggests one measurement is average of 10 readings
International Maritime Organization (IMO) Performance Standard for Protective Coatings (PSPC)
The measured profile should be between 30 and 75 microns
Surface profile test standards
US Navy NAVSEA Standard Item (NSI) 009-32
For the first 100 m2, one profile reading shall be taken for every 20 m2
For each additional area of 50 m2 or less, one profile reading shall be taken
For critically coated areas, profile readings shall be a minimum of 50 microns
For non critical areas the minimum is 25 microns

## Slide 29
Example – Calculating the number of measurements
  Consider a 100m2 area
  A mean value needs to be taken every 20m2
  _
  One mean profile value = 10 gauge measurements
  Total is 5 x 10 = 50 measurements
Paperless QA

## Slide 30
Example – Calculating the number of measurements
  Now expand this to 200m2
  For each additional area of less than 50m2 one profile mean value shall be taken
  Already have 5 mean values for the first 100m2
  Additional 2 mean values (1 per 50m2) required for a total of 7 mean values
  10 gauge measurements per reading
  70 Readings in total
Paperless QA

## Slide 31
Paperless QA
Workshop 1: Taking Surface Profile Measurements & Mean Values

## Slide 32: Paperless QA
and the Elcometer 224

## Slide 33
Connecting Gauges
  Elcometer gauges may be connected in 3 ways
Paperless QA
USB
RS232

## Slide 34: Paperless QA
Creating a Bluetooth connection
  All 224 top gauges come with Bluetooth built in
  Your PC requires Bluetooth as well in order to connect to the gauge
  Should your computer not have bluetooth, a USB bluetooth dongle may be used
A typical bluetooth USB adapter

## Slide 35: Paperless QA
Creating a Bluetooth connection
  Gauges must be “added” to the software before data can be downloaded
  Elcomaster will remember the gauge for quick downloads in future
  The “Download” screen is displayed by default
  All previously added gauges are displayed here

## Slide 36: Paperless QA
The connect gauge button opens the wizard to add a gauge

## Slide 37: Paperless QA
Creating a Bluetooth connection
  Click “connect gauge”
  Follow the wizard through, selecting the appropriate options for the Elcometer 224
  After Elcomaster 2.0 finds your gauge, add the correct one by checking the serial number in the bluetooth menu …. menu > Bluetooth
  Key in the Bluetooth PIN found on the same screen
  The gauge is now saved and data may be downloaded with

## Slide 38: Paperless QA
Data Storage
PROJECTS
Top level folder for
large of data
Folders
Divide up related
collections of data
Batches
Elcomaster 2.0
Database
Organising your data is simple
Elcomaster 2.0 makes it easy to effectively file your information away for later review

## Slide 39: Paperless QA
Simple Reporting in Elcomaster 2.0
  Elcomaster 2.0 already contains a very simple report template function
  If a client doesn’t have Elcomaster 2.0 then it can be used to send a simple summary of the data by email
  Select a batch in the “View” screen and select “PDF” from the bar across the top
  The key parts are “batch summary” and “batch readings” but other features can be added too
  Your company logo can be added to this in settings/report
Notes: 39

## Slide 40: Paperless QA
Downloading Data and Simple Reporting Walkthrough
Viewing Batches
Creating a simple pdf report
Exporting data to excel
Adding a company logo to the simple report

## Slide 41: Paperless QA
Benefits of Paperless QA
Surface Profile

## Slide 42: Paperless QA
The number of readings that have to be collected builds up
quickly on large structures
  A large ship has a surface area to be coated of 58,000m2
  First take readings for the first 100m2, 1 per 20m2 = 5 mean values
  The next 57,900m2 are divided up into 50m2 sections with one mean value in each
  1158 readings plus the original 5 is 1163 readings
  Ten measurements per mean value = 11,630 measurements in total
  A vast amount of data is created
  Time taken would stretch into days of work for an inspector over the course of the job

## Slide 43: Paperless QA
How Elcomaster 2.0 can help
  Organise the data using batches
  Save time transcribing readings onto paper
  Store the readings in an organised way for easy review later
  Store data safely and securely using cloud technology
  Create customised, professional reports in seconds using Elcomaster 2.0

## Slide 44: Paperless QA
Summary
  The Elcometer 224 is designed to measure profiles created by abrasive blast cleaning
  Creating a suitable surface profile is key to coating adhesion and longevity
  The Elcometer 224 is used by taking several readings in an area to get a spot measurement
  Standards can be used to help determine how many readings to take and optimum blast profile

## Slide 45: Paperless QA
What have we learned so far?
  A broad understanding of Profile and Roughness Measurement techniques
  How to use the Elcometer 224 Profile Gauge
  How to create and store a counted average profile batch to speed up data collection when working to a standard
  How to connect the Elcometer 224 gauge to Elcomaster 2.0
  How to create a simple inspection report
  This is the basis of PQA

## Slide 46: Paperless QA
Salt Contamination Testing
Using the Elcometer 130

## Slide 47
Measuring Salt Contamination
Chloride Salts are not uniformly spread across a surface
Salt ‘Mountains’ form by ionic bonding
Salt ‘Deserts’ form as a result of the ‘mountains’
Measuring Chloride Salts is a complex science and requires a deeper understanding of the real conditions
Measurement techniques work more reliably when testing larger areas
Multiple Tests are therefore required
.

## Slide 48
Presence of soluble salts on a surface causes corrosion to greatly accelerate and reduces the serviceable lifespans of protective coatings
Soluble salts that contaminate a surface are typically invisible, therefore some method of testing must be performed to determine if such contamination exists
The salts stimulate corrosion by drawing moisture through the coating
Paperless QA

## Slide 49: Paperless QA
Moisture, when combined with chlorides, actually often forms a mild hydrochloric acid. This causes corrosion, undercutting of the coating and, finally, a coating failure
The U.S. Navy has adopted an acceptable level of <3 micrograms/cm2 for hulls below the water line, and many coating manufacturers are rewriting surface preparation specifications that require soluble salts be tested for and limited to certain levels.

## Slide 50: Paperless QA
The Elcometer 130 is designed to detect the level of soluble salts on a surface

## Slide 51: Paperless QA
Specially cleansed filter papers are dosed
with pure water
Filter paper placed on surface for 2 minutes
Removed and placed into Elcometer 130 for
analysis
Filter papers can be halved or quartered
and dosed accordingly
Automatic paper size detection

## Slide 52: Paperless QA
USB and Bluetooth output to Elcomaster
Batch memories on top model
Upto 150,000 readings in 2,500 batches
Results measured in µg/cm2
Additional units in top model
  ppm µS/cm mS/cm % Salinity mg/m²
Bluetooth on top model only

## Slide 53: Paperless QA
Elcometer 130 Walkthrough

## Slide 54: Paperless QA
What have we learned so far?
  A broad understanding of Salt Contamination Measurement techniques
  How to use the Elcometer 130 SCM
  How to create and store a batch to speed up data collection
  How to download Salt Contamination data into Elcomaster 2.0
  How to create a simple inspection report

## Slide 55: Paperless QA
Climatic Testing
Using the Elcometer 319

## Slide 56: Paperless QA
Module Objectives
  Define ambient conditions
  Define the ambient condition coating requirements of related industry standards
  Measure the ambient conditions using a digital dewpoint meter

## Slide 57: Paperless QA
Ambient Conditions
  The climatic conditions at a given place and time
    Air temperature
    Relative humidity
    Dew point temperature
    Wind velocity
  Conditions must be monitored on the job site

## Slide 58
What effect do the climatic conditions have?
Paperless QA

## Slide 59
Relative Humidity
  A ratio of the amount of moisture in the air at a given temperature to the maximum amount of water that the air at that temperature can hold expressed as a percentage
  At 100% RH water cannot evaporate - the air is full of water
  Direct effects
Paperless QA
RH too low
RH too high

## Slide 60
Temperature readings Ta and Ts
  Ta – Air temperature
  Ts – Surface temperature
  Most coatings will have a range of temperatures over which they may be applied. Generally it must be at least 12°C to paint
  Direct effects
Paperless QA
Ts or Ta too high
Ts or Ta too low

## Slide 61
Dew Point Temperature
  Indirect effect on coating performance
  The temperature at which the moisture in the air condenses as water
    Steam on a cold glass window
    or moisture on the outside of a cold drink
  When air is cooled, the amount of water it can hold decreases
Paperless QA
Dew on a cold bottle
Notes: What happens if the air is at 100%RH and then it cools?

## Slide 62
Dew Point Temperature
  Dew is of concern to coating contractors and paint inspectors
  Presence of water on a surface detrimental effect on coating performance
    Prevents good adhesion
    Poor surface finish (blistering etc)
    Premature substrate corrosion
  Invisible “micro beads” of dew may be there if steel surface close to dewpoint
Paperless QA

## Slide 63
Dew Point Temperature
  There may be localised dew formation
  Dew may be formed in shaded areas as they are cooler
  Measurements should be taken in several locations to ensure surface is clear of micro beads prior to coating
Paperless QA

## Slide 64
Paperless QA
Delta T (ΔT)
  Difference between surface and dewpoint temperature
  Must be greater than 3°C to paint
Other measurements
  Dry bulb temperature and wet bulb temperature
  Measurements taken by the whirling hygrometer; used to calculate humidity and dewpoint
Notes: Kept these in because of the San Francisco Bridge application

## Slide 65
  Measures
    Surface temperature
    Relative humidity
    Air temperature
  Calculates
    Dew point temperature
    Delta T
    Wet Bulb Temperature
Paperless QA
Elcometer 319 Dewmeter
Notes: 65
This image shows the effect of the different cutter angles on the same thickness of coating.

## Slide 66
Paperless QA
  Displays 5 different parameters
  Sensors integrated into a tough drop and water resistant enclosure
  Special components allow functionality up to 80C
  Top gauge features large memory for paperless QA inspections
Elcometer 319 Dewmeter

## Slide 67
Paperless QA
  Controlled using 4 “softkeys”
  Function changes depending on gauge screen
  Word or symbol above each key indicates function at that time
Operating the gauge
Notes: 67

## Slide 68
Paperless QA
  The hold key freezes whatever is on the display
  In batch mode, a save option is also provided
Operating the gauge
Notes: 68

## Slide 69
Paperless QA
  Two types of data logging
    Manual logging batch: The gauge will save a reading when the hold and save function is used. A batch must be open for the data to be saved
    Interval logging batch: The gauge saves readings at programmed time intervals
Batching
Notes: 69

## Slide 70
Walkthrough:
Using the Elcometer 319
Operation
Measurement
Statistics
Batching
Limits
Manual and Interval Logging

## Slide 71
Paperless QA
Workshop 2:
Manual and Interval Logging
Live Readings
Combined Batches
Combined Reports

## Slide 72: Paperless QA
Summary
  To avoid premature coating degradation, coatings should only be applied under optimum climatic conditions. Typical conditions
    Relative humidity under 85%
    Surface temperature above 12°C
    The surface temperature is at least 3 °C above the dewpoint
  The Elcometer 319 can be used to measure and record all climatic conditions simultaneously
  The interval logging function on the gauge may be used to reduce the workload on inspectors and save time

## Slide 73: Paperless QA
What have we learned so far?
  An understanding of Climatic Condition Measurement techniques
  How to use the Elcometer 319 Dewmeter
  How to create and store a batch in the gauge to speed up data collection
  how to create an inspection report with combined attributes
  How to create a more detailed inspection report

## Slide 74: Paperless QA
Measuring with a DFT Gauge
The Elcometer 456

## Slide 75: Paperless QA
Module Objectives 1
  What is Dry Film Thickness
  Substrates & coatings
  Instrument types – E,B,S,T
  Smooth and Rough Surface Gauge Calibration Techniques
  80/20 and IMO 90/10 rules

## Slide 76: Paperless QA
Module Objectives 2
  Elcometer 456 Batch Types
  Elcometer 456 Probes and Scales
  Elcometer 456 Scan Probes

## Slide 77: Paperless QA
Definition – Dry Film Thickness
The thickness of a dry paint layer on top of a substrate
Often expressed in microns but for thicker coatings millimetres is sometimes used

## Slide 78
What is Calibration
Calibration is an adjustment made to a gauge by the user before measurement
Calibration should be carried out:
  At the start of each shift
  When the base material type changes
  When the nominal coating thickness changes
  When the shape of the base material changes
Correct calibration ensures best accuracy and instrument performance
Wherever possible calibrate on an uncoated sample of the same material
Paperless QA
Notes: 78
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 79
What is Calibration
A calibration certificate for the gauge or probe cannot be provided by the manufacturer
  A test certificate is available
If the manufacturer calibrates and the first thing the user does is recalibrate it to their job the manufacturer calibration is lost
Paperless QA
Notes: 79
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 80
What is Calibration
Instead we provide a calibration certificate for the tools the user uses for calibration
Calibration Shims
A certificate for the shims is traceable to international standards
Paperless QA
Notes: 80
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 81
Calibration Shims
  Shims (or foils) are provided with every gauge
  Shims are accurately measured standards, certificates are available
  Shims allow a gauge’s accuracy to be verified
  Shims allow a gauge to be adjusted to be best suited to the current job
Paperless QA
Notes: 81
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 82
Paperless QA
Accuracy Verification
  Gauges and their probes should regularly have their accuracy verified
  Use a smooth “zero plate”
  Calibrate between a range
  Test the gauge on some shims in between
  If outside of accuracy statement recalibrate
Notes: 82
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 83
Paperless QA
Accuracy Verification
  Record data on:
    Serial number
    Reference standard used (foil and zero plate serial number)
    Foil Thicknesses
    Calibration method
  The stated thickness of the standard and the measured value should be recorded. Check tolerances
Notes: 83
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 84
Paperless QA
Calibration Methods
  Smooth surfaces
  Blasted surfaces – Rough and 2-point calibration
  Smooth Surface with Base Metal
  Reading compensation (SSPC method)
Notes: 84
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 85
Paperless QA
Calibration – Smooth Surfaces
  Carry out on an unblasted smooth surface
  Requires one calibration foil and a zero reference
  Choose a foil or combination of foils that is slightly greater than the expected coating thickness
Stacked Foils
Notes: 85
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 86
Paperless QA
Smooth Surface Calibration Demo
Notes: 86
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 87
Paperless QA
So we have some shims to calibrate with, but they’re not the same material as the paint.
How can this work?
Notes: 87
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 88
Calibration – Why you can measure almost any coating on steel
Paperless QA
Magnetic Substrate
Substrate
Non-magnetic coating
Air Gap
Probe
Probe
Notes: 88
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 89
Ferrous Calibration – Why you can measure almost any coating on steel
Paperless QA
Magnetic Substrate
Magnetic Substrate
Non-magnetic coating
Air Gap
The gauge measures from the probe tip to the substrate
Except for a few rare cases what is in between makes no difference
Probe
Probe
Notes: 89
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 90
Non-Ferrous Calibration – Why you can measure almost any coating on other metals
Paperless QA
Metal Substrate
Metal Substrate
Non-conductive coating
Air Gap
Non Ferrous gauges are similar
The coating must be an electrical insulator
Probe
Probe
Notes: 90
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 91
Paperless QA
Calibration – Rough Surfaces
  Most protective coatings are applied to abrasively blasted surfaces
  DFT specification should be coverage from the peaks of the profile to ensure all steel is effectively covered
  Thickness measured will be the minimum – ensures proper coverage
Notes: 91
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 92
Paperless QA
Calibration on Rough Surfaces - The Problem
  Where do we take the zero
  Using a smooth calibration the zero could be anywhere, depends where the probe lands
Location of zero
Notes: 92
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 93
Paperless QA
Calibration on Rough Surfaces - The Problem
  Where do we take the zero
  Using a smooth calibration the zero could be anywhere, depends where the probe lands
Location of zero
Notes: 93
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 94
Paperless QA
Calibration foil
Calibration on Rough Surfaces - Solution #1
  If we use two calibration foils instead of a zero, the problem of moving zero is eliminated
  The thin calibration foil bridges the profile
  A second, thick calibration foil is also used
  The gauge is accurate between these two values
Location of zero
Notes: 94
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 95
Paperless QA
2-Point (Rough) Calibration Demo
Notes: 95

## Slide 96: Paperless QA
Calibration on rough surfaces
Solution #2
  The ISO 19840 standard specifies a method to compensate for the effect of blast profile on the reading
  The Base metal reading (BMR) method
  The profile is categorised as fine, medium or coarse according to ISO 8503 and then a figure is subtracted from the gauge reading

## Slide 97: Paperless QA
Measuring paint on blasted surfaces
ISO 8503 Profile Grade | Correction Value (µm) | Correction Value (mil)
Fine | 10 | 0.4
Medium | 25 | 1.0
Coarse | 40 | 1.6
  The SSPC-PA 2 Standard provides approximate BMR values that can be used when access to the blast-cleaned surface is not possible.

## Slide 98: Paperless QA
Calibration on blasted surfaces 2
  Select zero offset cal method and set offset to required value
  Calibrate on a flat steel plate (unblasted)
  Measure as normal, create counted average batches with appropriate number of readings based on the standard

## Slide 99
Paperless QA
Batching on the 456 Demo
Creating Batches
Naming Batches
Counted Average and Fixed Batches
Auto Repeat and Scan Batches
Notes: 99
The Elcometer 456 is the most popular of the Elcometer coating thickness gauges.
It is available as Basic, Standard or Top software options with either integral or separate probes and F, N or dual FNF operation.
This is the Elcometer philosophy of Customer choice in operation.

## Slide 100: Paperless QA
80/20 Rule
Values above NDFT
Increasing thickness
Values 80+% of NDFT
Values below 80% of NDFT
Instant Fail
NDFT

## Slide 101: Paperless QA
80/20 Rule
Values above NDFT
Increasing thickness
Values 80+% of NDFT
Values below 80% of NDFT
Instant Fail
Above upper limit set by coating manufacturer
NDFT

## Slide 102: Paperless QA
IMO PSPC Regulations
  Stipulate an NDFT or Nominal Dry film Thickness
  NDFT for ballast tank coating is 320 microns
  Use a 90/10 rule to determine pass or fail criteria
  Measurement frequency and procedure determined by ISO 19840

## Slide 103: Paperless QA
IMO PSPC Regulations
  IMO PSPC provides guidance on where to measure on steel supporting members in ballast tanks
  Example

## Slide 104: Paperless QA
90/10 Rule
Values above NDFT
Increasing thickness
Values 90+% of NDFT
Values below 90% of NDFT
Instant Fail
Above upper limit set by coating manufacturer
NDFT

## Slide 105: Paperless QA
  Using the features of the Elcometer 456 DFT gauge to work to the standards

## Slide 106: Paperless QA
Counted averages
  Counted average batches can be used to aggregate your spot readings into average measurement
  Set number of readings to become a measurement
  Gauge saves and notifies average when spot measurement complete
  Useful for working with ISO 19840

## Slide 107: Paperless QA
IMO PSPC Batches
  Set the NDFT to the desired thickness
  IMO PSPC dynamic statistics displayed on screen
  Immediate indication of pass/fail on IMO PSPC regulations

## Slide 108: Paperless QA
  Workshop 6: 456 Extension exercise
  Limits, counted average and fixed batch

## Slide 109: Paperless QA
What have we learned?
  Correct dry film thickness measurement is essential to coating performance
  Gauge accuracy can be verified using calibration foils
  Standards are available as a guide to the measurement process
  Correct gauge and software set up can save time and money

## Slide 110: Coating Inspection Data Management and Reporting

## Slide 111: Coating Inspection – Trends
The need for coating inspection is driven by Project Specifications
  These specifications determine
    The type coating to be applied
    The film thickness to be achieved
    The National/International Standard to use to determine the coating thickness

## Slide 112: Coating Inspection – Trends
Coating thickness has always been seen as critical in Corrosion prevention
However we see other factors are increasingly being recognised as critical to the successful application of a coating and the prevention of corrosion

## Slide 113: Coating Inspection – Trends
Project specifications are requiring inspection at all key stages of the application process
    Surface Profile
    Surface Cleanliness
    Climatic Conditions
    Dry Film Thickness
    Adhesion

## Slide 114: Coating Inspection – Trends
The coatings market is demanding:
  Increased inspection through the whole application process
  Proof that inspections were completed

## Slide 115: Coating Inspection – Trends
Proof of inspection requires Reports
Reports require data
    Simple visual assessments
    Multiple Readings/Measurements
    Statistics
    Analysis

## Slide 116: Coating Inspection – Trends
The volume of data/measurement is increasing
Trend is for electronic data capture over manual/hand written/paper based inspection

## Slide 117: Coating Inspection - Trends
Equipment to record data must be
    Rugged
    Accurate/Reliable
    Calibrated/Certified
    Batch Memory/Time & Date Stamped
    Traceability/Serial Number

## Slide 118: Coating Inspection – Elcometer Solution
Elcometer have developed a range of gauges in response to these market demands

## Slide 119: Data Collection – Elcometer Solution
Surface Profile
    Elcometer 224 Surface Profile Gauge
      150,000 readings / 2,500 batches
      50+ readings/minute
      Rated to IP64
      Bluetooth® connectivity
      USB connectivity
      Compatible with ElcoMaster™

## Slide 120: Data Collection– Elcometer Solution
Surface Cleanliness
    Elcometer 130 Salt Contamination Meter
      150,000 readings / 2,500 batches
      Measuring range up to 50μg/cm
      Rated to IP64
      Bluetooth® connectivity
      USB connectivity
      Compatible with ElcoMaster™

## Slide 121: Data Collection– Elcometer Solution
Climatic Conditions
    Elcometer 319 Dewpoint Meter
      25,000 readings / 999 batches
      Measuring RH%, Ta,Ts, Td and TΔ
      Rated to IP66
      Bluetooth® connectivity
      USB connectivity
      Compatible with ElcoMaster™

## Slide 122: Data Collection– Elcometer Solution
Dry Film Thickness
    Elcometer 456 Dry Film Thickness Gauge
      150,000 readings / 2,500 batches
      70+ readings/minute
      Rated to IP64
      Bluetooth® connectivity
      USB connectivity
      Compatible with ElcoMaster™

## Slide 123: Data Management – Elcometer Solution
  To organise the volumes of data collected during inspections Elcometer have developed:
  ElcoMaster™ 2.0 Software – PC and Laptop
  ElcoMaster™ Mobile Software - tablet/mobile phone
  Provides one standard platform for all Elcometer gauges
  USB/Bluetooth®/Cloud/email/Live data

## Slide 124: Data Management – ElcoMaster™ 2.0
Developing ElcoMaster™ Software
  Elcometer looked at other software products in the market
  We based the visual appearance and data structure on email applications
  We designed a ‘one click’ intuitive menu based on Satellite Navigation products

## Slide 125: Data Management – ElcoMaster™ 2.0
Visual appearance and data storage based on email applications

## Slide 126: Data Management – ElcoMaster™ 2.0
Data is organised in to Projects/Folders/Batches – all details of the batch can be seen
1
2
3
4

## Slide 127: Data Management – ElcoMaster™ 2.0
The intuitive menu design based on Satellite Navigation products
  Wherever possible all ‘actions’ within ElcoMaster™ are ‘one click’ operations
  Wizards guide the user through key operations

## Slide 128: Data Management – ElcoMaster™ 2.0
Downloading data via Bluetooth® or USB is a ‘one click’ operation
1
2

## Slide 129: Data Management – ElcoMaster™ 2.0
Wizard guides user to store data in required location:
1
2

## Slide 130: Data Management – ElcoMaster™ 2.0
ElcoMaster™ Software Summary
    Key features include:
    PC, Tablet and Mobile phone software options
    USB/Bluetooth®/Cloud/email/Live data connectivity
    Three operating modes: Microsoft Excel/Standard/Advanced
    One platform – connects all Elcometer (memory) gauges
    Easy download of data
    Instant archiving of data
    Data organised into Projects/Folders
    Standardised reporting templates – limited customisation possible
    Labels – Customised Project & Batch labels can be added
    Photographs can be added to batches (unlimited)
    Design reporting templates – full customisation possible
    PDF based software – PDF exported and any PDF can be imported

## Slide 131: Data Management – ElcoMaster™ 2.0
We will now look at some of the features of
ElcoMaster™ 2.0

## Slide 132: Data Management – ElcoMaster™ 2.0
ElcoMaster™ – Settings: Language
1

## Slide 133: Data Management – ElcoMaster™ 2.0
ElcoMaster™ – Settings: Mode

## Slide 134: Data Management – ElcoMaster™ 2.0
ElcoMaster™ – Settings: Units

## Slide 135: Data Management – ElcoMaster™ 2.0
ElcoMaster™ – Settings: Report
2
1

## Slide 136: Data Management – ElcoMaster™ 2.0
ElcoMaster™ – Settings: Storage
1
2

## Slide 137
Connecting Gauges
“Pairing”

## Slide 138: Data Management – ElcoMaster™ 2.0
Connecting/Pairing Gauges – Connect Gauge Wizard
1
2

## Slide 139: Data Management – ElcoMaster™ 2.0
Connecting/Pairing Gauges – Select connection
1

## Slide 140: Data Management – ElcoMaster™ 2.0
Connecting/Pairing Gauges – Enter Bluetooth® code
1
2

## Slide 141: Data Management – ElcoMaster™ 2.0
Connecting/Pairing Gauges – Gauge paired

## Slide 142
Download Data
From Gauges

## Slide 143: Data Management – ElcoMaster™ 2.0
Download data - select gauge/download method
2
1

## Slide 144: Data Management – ElcoMaster™ 2.0
Select download destination – ElcoMaster™ 2.0 File

## Slide 145: Data Management – ElcoMaster™ 2.0
From Project list – select existing project or ‘new’
1
2

## Slide 146: Data Management – ElcoMaster™ 2.0
Download complete – Finish to see data
1
2

## Slide 147: Data Management – ElcoMaster™ 2.0
Instant visibility of Batch Data details

## Slide 148
Organising Data
Into Projects

## Slide 149: Data Management – ElcoMaster™ 2.0
All batch data files can be organised into
  Projects
  Folders

## Slide 150: Data Management – ElcoMaster™ 2.0
So what is a “Project”?
  A major construction:
    Ship
    Pipeline
  A key account/customer:
    Acme Windows
  A production line in the factory:
    Line 1 - panels
    Line 2 - boxes

## Slide 151: Data Management – ElcoMaster™ 2.0
Example construction project
HMS Elcometer
  Project data organised into :
  Location Folders
    Zones
  Document Folders
    Imported PDF files

## Slide 152: Data Management – ElcoMaster™ 2.0
Example key account project
Acme Windows
  Batch data organised into :
  Year Folders
    Product Folders
      Contract Folders

## Slide 153: Data Management – ElcoMaster™ 2.0
Example production line project
Production Line 1
  Batch data organised into:
  Product Folders
    Year Folders
      Month Folders

## Slide 154
Download Elcometer 456 Batch: BT 1 28.8.13
to a project

## Slide 155: Data Management – ElcoMaster™ 2.0
Use download wizard
Select Project
  HMS Elcometer
Select Location
  Ballast Tank 1

## Slide 156: Data Management – ElcoMaster™ 2.0
  - HMS Elcometer/Ballast Tank 1/Batch BT 1 28.8.13

## Slide 157: Data Management – ElcoMaster™ 2.0
Other information can be added to Projects
  Labels – Project & Batch
  Photographs
  PDF documents

## Slide 158
Adding
Project & Batch
Labels

## Slide 159: Data Management – ElcoMaster™ 2.0
Select a Project – Label input screen visible
  All labels are defined by the user
  3 Project labels can be added – universal to project reports
  5 Batch labels can be added – specific to batch reports

## Slide 160: Data Management – ElcoMaster™ 2.0
Input Project/Batch Labels
  All labels are defined by the user
  3 Project labels can be added – universal to project report
  5 Batch labels can be added – specific to batch report

## Slide 161: Data Management – ElcoMaster™ 2.0
Input Project/Batch Labels
  These labels will be printed on all Project and Batch reports

## Slide 162
Adding
Batch Photographs

## Slide 163: Data Management – ElcoMaster™ 2.0
Adding Batch photographs
1
2
3
4

## Slide 164: Data Management – ElcoMaster™ 2.0
Adding Batch photographs – unlimited number

## Slide 165
Adding
PDF Documents

## Slide 166: Data Management – ElcoMaster™ 2.0
ElcoMaster™ exports all Project and Batch Reports as PDF files
ElcoMaster™ will also import PDF files
  Product Datasheets
  Word documents
  CAD drawings
  Hand written forms

## Slide 167: Data Management – ElcoMaster™ 2.0
Adding PDF Documents – Select Project/Folder
1
2
3

## Slide 168: Data Management – ElcoMaster™ 2.0
Unlimited number of documents can be added

## Slide 169
Creating Reports

## Slide 170: Data Management – ElcoMaster™ 2.0
All reports are generated as PDF Files
A variety of reports can be produced from a simple one page summary of one Batch to a full multi-page Project report

## Slide 171: Data Management – ElcoMaster™ 2.0
Producing Batch reports – ‘Summary’ sheet
2
1
3

## Slide 172: Data Management – ElcoMaster™ 2.0
Producing Batch reports – ‘Summary’ PDF

## Slide 173: Data Management – ElcoMaster™ 2.0
Batch Report – Summary Page
1
2
3

## Slide 174
Adding Notes
To Batch Reports

## Slide 175: Data Management – ElcoMaster™ 2.0
Select Batch – Notes
1
2
3

## Slide 176: Data Management – ElcoMaster™ 2.0
Producing Batch reports – Additional pages
1
3
2

## Slide 177: Data Management – ElcoMaster™ 2.0
Batch Summary page, Batch Photo, Batch readings

## Slide 178: Data Management – ElcoMaster™ 2.0
Batch Summary Page

## Slide 179: Data Management – ElcoMaster™ 2.0
Batch Photographs

## Slide 180: Data Management – ElcoMaster™ 2.0
Batch Readings

## Slide 181
Project Reports

## Slide 182: Data Management – ElcoMaster™ 2.0
Folder reports – all batches included
1
2

## Slide 183: Data Management – ElcoMaster™ 2.0
Project reports – all folders/batches included
2

## Slide 184
Emailing Reports

## Slide 185: Data Management – ElcoMaster™ 2.0
Producing Reports – via email
1
2
3

## Slide 186: Data Management – ElcoMaster™ 2.0
Producing Reports – via email
1
2
3

## Slide 187
Live Data Input
Collect Batches
(Image)

## Slide 188: Data Management – ElcoMaster™ 2.0
“Collect” reports use photos/images with the measurement points highlighted on the image to tell the user where to take measurements
Requires live data input using USB or Bluetooth®

## Slide 189
Design
Collect Batches

## Slide 190: Data Management – ElcoMaster™ 2.0
Design Collect – Select ‘New’ opens design wizard
1
3
2

## Slide 191: Data Management – ElcoMaster™ 2.0
Design Collect – Select Report Type

## Slide 192: Data Management – ElcoMaster™ 2.0
Design Collect – Select Report Image from file
1
2
3

## Slide 193: Data Management – ElcoMaster™ 2.0
Design Collect – Select the number of readings
1

## Slide 194: Data Management – ElcoMaster™ 2.0
Design Collect – Locate the points on the image
1
2

## Slide 195: Data Management – ElcoMaster™ 2.0
Design Collect – Save the Collect Report

## Slide 196
Use
Collect Batches
(Image)

## Slide 197: Data Management – ElcoMaster™ 2.0
View: Project/Folder – Open new ‘Turkcoat 2013’

## Slide 198: Data Management – ElcoMaster™ 2.0
Collect/Live Data – Connect gauge
1
2

## Slide 199: Data Management – ElcoMaster™ 2.0
Collect/Live Data – Select gauge
1
2

## Slide 200: Data Management – ElcoMaster™ 2.0
Collect/Live Data – Turkcoat 2013 ready
2
1

## Slide 201: Data Management – ElcoMaster™ 2.0
Collect/Live Data– Readings displayed at location
2
1

## Slide 202: Data Management – ElcoMaster™ 2.0
Collect/Live Data – 3 units measured
1
2

## Slide 203
Creating
Collect Batch
Reports

## Slide 204: Data Management – ElcoMaster™ 2.0
Select PDF – Select ‘Collections’

## Slide 205: Data Management – ElcoMaster™ 2.0
Turkcoat 2013 Batch Report – P1 of 5
1

## Slide 206: Data Management – ElcoMaster™ 2.0
Turkcoat 2013 Batch Report – P2 of 5
1

## Slide 207: Data Management – ElcoMaster™ 2.0
Turkcoat 2013 Batch Report – P3 to 5
1

## Slide 208
ElcoMaster™ Mobile App

## Slide 209: Data Management – ElcoMaster™ App
ElcoMaster™ 2.0 links with ElcoMaster™ Mobile App
  Android platform
    Laptop
    Tablet
    Mobile phone
    Bluetooth®
    Cloud

## Slide 210: Data Management – ElcoMaster™ 2.0
Mobile App

## Slide 211: Data Management – ElcoMaster™ 2.0
Mobile App

## Slide 212: Data Management – ElcoMaster™ 2.0
Mobile App
  Connect Gauge
    Select Device Menu

## Slide 213: Data Management – ElcoMaster™ 2.0
Mobile App
  Connect Gauge

## Slide 214: Data Management – ElcoMaster™ 2.0
Mobile App
  Connect Gauge

## Slide 215: Data Management – ElcoMaster™ 2.0
Mobile App
  New Batch
    Select Device Menu

## Slide 216: Data Management – ElcoMaster™ 2.0
Mobile App
  New Batch
1
2

## Slide 217: Data Management – ElcoMaster™ 2.0
Mobile App
  New Batch
    Added to list

## Slide 218: Data Management – ElcoMaster™ 2.0
Mobile App
  Review Batch

## Slide 219: Data Management – ElcoMaster™ 2.0
Mobile App
  Review Batch
    Header
1
2
3
4

## Slide 220: Data Management – ElcoMaster™ 2.0
Mobile App
  Review Batch
    Readings
1
2
3

## Slide 221: Data Management – ElcoMaster™ 2.0
Mobile App
  Review Batch
    Graph
    Chart
1
2
3

## Slide 222: Data Management – ElcoMaster™ 2.0
Mobile App
  Review Batch
    Add Photo(s)
1
2
3

## Slide 223: Data Management – ElcoMaster™ 2.0
Mobile App
  email
1

## Slide 224: Data Management – ElcoMaster™ 2.0
Mobile App
  email
    Long press batch
1
2

## Slide 225: Data Management – ElcoMaster™ 2.0
Mobile App
  email
1

## Slide 226: Data Management – ElcoMaster™ 2.0
Mobile App
  email
1
2
3
4

## Slide 227: Data Management – ElcoMaster™ 2.0
Receiving Reports via email from mobile device

## Slide 228: Data Management – ElcoMaster™ 2.0
Receiving Reports – via email from mobile device
Double click

## Slide 229: Data Management – ElcoMaster™ 2.0
Receiving Reports – via email from mobile device
Double click
Automatically opens ElcoMaster™ 2.0 to allow data input into Project Folder

## Slide 230: Data Management – ElcoMaster™ 2.0
Mobile App
  GPS Location
1

## Slide 231: Data Management – ElcoMaster™ 2.0
Mobile App
  GPS Location
1
2

## Slide 232: Data Management – ElcoMaster™ 2.0
Mobile App
  GPS Location
    Long Press
1

## Slide 233: Data Management – ElcoMaster™ 2.0
Mobile App
  GPS Location
1

## Slide 234: Data Management – ElcoMaster™ 2.0
Mobile App
  GPS Location
    Google Maps
    Display reading
1

## Slide 235: Data Management – ElcoMaster™ 2.0
Mobile App
  GPS Location
    Long press
1
2

## Slide 236: Data Management – ElcoMaster™ 2.0
Mobile App
  GPS Location
    Google Map
    All readings

## Slide 237: Data Management – ElcoMaster™ 2.0
Mobile App
  Collect Batch
    Display readings on image
1

## Slide 238: Data Management – ElcoMaster™ 2.0
Mobile App
  Collect Batch
    Display readings on image
2
1

## Slide 239: Data Management – ElcoMaster™ 2.0
Mobile App
  Collect Batch
    Display readings on image
    Image focus on next reading
2
1

## Slide 240: Data Management – ElcoMaster™ 2.0
ElcoMaster™ 2.0
  Free download www.elcometer.com
  Free CD with all Elcometer Gauges
ElcoMaster™ Mobile
  Free at Google Play Store

## Slide 241
Thank You

## Slide 242: Paperless QA
Elcomaster 2.0 Appendix

## Slide 243: Paperless QA
CHARTS
  Elcomaster 2.0 can create line graphs or histograms of your data
  Useful for analysing trends in data
  Limits and statistical data can be added to the graph in the view section

## Slide 244: Paperless QA
Individuals Chart

## Slide 245: Paperless QA
Histogram with normal distribution curve

## Slide 246: Paperless QA
LABELS
  Include optional data on the data in your project
  Project labels apply to all batches
  Batch labels are options for each batch in the project
  Accessed and edited from the view screen

## Slide 247: Paperless QA
What can labels be used for
  Marking out different structures in a project
  Marking out different inspectors within a project
  Different physical locations
  Labels can be added to report templates later

## Slide 248: Paperless QA
Setting labels up
  Select a project from the view screen
  Add a project label with the green button
  Add a batch label below

## Slide 249: Paperless QA
Batch Labels
  When batches are added to a project, Elcomaster 2.0 will prompt for which label to apply
  Set the label options in the project
  Labels may be picked from a drop down list or manually typed in

## Slide 250: Paperless QA
BATCH PHOTOS
  Applying images to your batch allows quick identification of the gauge job in hand.
  Images can be attached to any simple report that you create

## Slide 251
Labels and Photos Demonstration
Paperless QA

## Slide 252: Paperless QA

## Slide 253: Paperless QA
What’s an Android
  Android is a common mobile phone operating system or OS
  Android allows you to run “Apps” or applications just like programs on a desktop PC
  Elcometer produce an Elcomaster App with many of the analysis features found on the desktop Elcomaster

## Slide 254: Paperless QA
Features
  Bluetooth connection to gauges
  Graphing, statistics
  Can use your device’s camera to attach a photo to a batch
  GPS location tagging
  Email batches from anywhere
  Integrate with the cloud and send your data to Elcomaster PCs or other Elcomaster mobile devices

## Slide 255
ElcoMaster 2.0
Cloud Computing

## Slide 256
Scenario
ElcoMaster 2.0
Cloud Computing
Inspection is taking place
Manual methods are the only way
How is the data stored and collected?
Here
Here
& Here

## Slide 257
ElcoMaster 2.0
Cloud Computing
Inspections are
being carried out at
all these locations
And you are inspecting
here
Imagine
and your PC is here

## Slide 258
Imagine
ElcoMaster 2.0
Cloud Computing
Components
Manufactured
are Assembled here
Here
Here
& Here

## Slide 259
ElcoMaster 2.0
Cloud Computing
Problem
  For progress reports between sites, individual reports had to be created and then emailed manually
  Sharing data between interested parties can be a time consuming process
  Transferring data between computers can be difficult enough

## Slide 260
ElcoMaster 2.0
Cloud Computing
ElcoMaster 2.0
Cloud Computing
ElcoMaster 2.0 and ElcoMaster for Android allows you to automatically:
  Synchronise data across multiple users and computers
  Share gauge information immediately anywhere in the world
  Link Elcomaster 2.0 and Elcomaster for Android so you need never visit the computer data is being sent to
Solution

## Slide 261
ElcoMaster 2.0
Cloud Computing
What is
Cloud Computing ?
Cloud Computing is
database storage on the web

## Slide 262
  ElcoMaster 2.0 supports several cloud service providers
  Elcometer do not have access to your data
  Data is held on the provider’s servers, protected by your own login credentials
ElcoMaster 2.0
Cloud Computing
Is it Independent?

## Slide 263
ElcoMaster 2.0
Cloud Computing
How does it work?
3G
3G

## Slide 264
ElcoMaster 2.0
Cloud Computing
How does it work?
3G
3G
Administrator
Limited Users

## Slide 265
ElcoMaster 2.0
Cloud Computing
Demonstration
3G
3G
Administrator
Limited Users

## Slide 266
ElcoMaster 2.0
Cloud Computing
Demonstration?

## Slide 267: Paperless QA
Creating Paperless QA reports with Elcomaster 2.0

## Slide 268: Paperless QA
Report Design
  Elcomaster 2.0 report designer is a major update from Elcomaster 1
  Accessed using “Design Report”

## Slide 269: Paperless QA
Report Design
  Elcomaster 2.0 report designer is a major update from Elcomaster 1
  Available templates listed under “Design report”

## Slide 270: Paperless QA
New Design
  Opens the new design wizard
  Any settings here may be changed later
  Choose the number and type of batches to go on the sheet
  Elcomaster 2.0 will handle any combination of material thickness, profile, climate and DFT batches in a single report

## Slide 271: Paperless QA
Report Items – Drag and Drop
  Elcomaster uses a “drag and drop” interface to build reports
  Boxes are positioned on the report template where you want data to appear
  Any data or gauge information can be placed on the report with the appropriate box
  Other boxes may be used to include additional user generated information

## Slide 272: Paperless QA
The four data box types
  Standard report items
    Manual entry, appears on every report
  Batch items
    Any information that can be downloaded from the gauge
  Manual entry items
    Areas that may be edited for each separate report
  Calculation report items
    Performs simple calculations on any other box item

## Slide 273: Paperless QA
Notes: From the basic elements you can create complex reports like this
Calculations are the % above the NDFT or % below the NDFT

## Slide 274: Paperless QA
Formatting Simple Boxes
  Boxes are formatted and adjusted by double clicking
  The report item property editor is displayed
  Examples

## Slide 275: Paperless QA
Formatting Boxes – Text Entry

## Slide 276: Paperless QA
Formatting Boxes – Text Entry 2

## Slide 277: Paperless QA
Formatting Boxes – Batch Readings

## Slide 278: Paperless QA
Formatting Boxes – Batch Readings 2

## Slide 279: Paperless QA
Calculation Boxes
Use different calc boxes for each operation – Can be chained together

## Slide 280: Paperless QA
Workshop 7: Recreating the simple report
Notes: 280

## Slide 281: Paperless QA
Backgrounds
  Your report may be created from scratch on blank pages
  Alternatively a pdf or jpeg image file background may be used
  Example SSPC QCS 2-07
    Available as free download from the Elcometer database

## Slide 282: Paperless QA
Notes: From the basic elements you can create complex reports like this
Calculations are the % above the NDFT or % below the NDFT
282

## Slide 284: Paperless QA
Practice – Creating a report by filling in a pdf document
  You will be provided with a pdf document of a report and some instructions on how to fill it in
  Use Elcomaster 2.0 to fill in at least one section of the report.
  Drag and drop a batch into the report to populate the boxes
  What happens if the batch is too big for the number of boxes created?